Supporting Information

Effect of Hydrogen-Bonding Networks of Water on Temperature and Relative Humidity Dependence of Proton Conductivity in Metal-Organic Frameworks

My V. Nguyen,§a,e Hieu C. Dong,§a,b Duc Nguyen-Manh,c Nam H. Vu,b,d  Thuat T. Trinhf  and Thang B. Phan*a,b

aCenter for Innovative Materials and Architectures (INOMAR), Ho Chi Minh City, Vietnam.

bVietnam National University-Ho Chi Minh (VNU-HCM), Ho Chi Minh City, Vietnam.

cCulham Centre for Fusion Energy, United Kingdom Atomic Energy Authority, OX143DB, Abingdon, UK

dFaculty of Materials Science and Technology, Ho Chi Minh City, Vietnam

eHo Chi Minh City University of Education, Ho Chi Minh City, Vietnam

fDepartment of Civil and Environmental Engineering, Norwegian University of Science and Technology, S.P Andersen vei 5, 7491-Trondheim, Norway

§These authors contributed equally

*To whom correspondence should be addressed:

pbthang@inomar.edu.vn

Section S1. Characteristics of MOF-801

Figure S1. FT-IR spectra of activated MOF-801 (black) and activated MOF-801 after exposure in air (red).

Figure S2. PXRD pattern of MOF-801 (black) in comparison with pelletized MOF-801 (red).

Figure S3. PXRD pattern of pelletized MOF-801 (black) in comparison with pelletized MOF-801 in water for 1 month (red) and in boiling water for 1 month (blue)

Section S2. Proton Conduction Study

It is noted that the impedance of the electric wire without pelleted sample was collected in order to correct for the inductive effect. The correction was carried out by subtracting the experimental impedance of pelletized sample from the experimental impedance of the electric wire in order to obtain the pure impedance of pelletized sample.

Figure S4. An equivalent circuit used for fitting. Schematic representations: W1, Warburg diffusion element; Q1/Q2, imperfect capacitor; R1, Contact resistor; R2, bulk resistor; R3, grain boundary resistor.

Figure S5. Nyquist plot derived from equivalent circuit (black line) and experimental Nyquist plot (red circles) of pelletized MOF-801 under 98% RH and 80 °C. Frequency ranged from 1 MHz to 10 Hz.

Table S1. Conductivity of pelletized MOF-801 at 50 oC from 60 to 98% RH.

| Relative humidity (%) | σ (S cm-1) |
| --- | --- |
| 60 | 4.49 x 10-8 |
| 70 | 2.08 x 10-7 |
| 80 | 6.01 x 10-7 |
| 90 | 1.53 x 10-6 |
| 95 | 2.08 x 10-5 |
| 98 | 8.84 x 10-4 |

Figure S6. Nyquist plot of pelletized MOF-801 at 50 °C under relative humidity varied from 60 to 98 %RH

Table S2. Conductivity of pelletized MOF-801 at 60 oC from 60 to 98% RH.

| Relative humidity (%) | σ (S cm-1) |
| --- | --- |
| 60 | 8.84 x 10-8 |
| 70 | 4.55 x 10-7 |
| 80 | 1.12 x 10-6 |
| 90 | 3.56 x 10-6 |
| 95 | 2.40 x 10-5 |
| 98 | 1.05 x 10-3 |

Figure S7. Nyquist plot of pelletized MOF-801 at 60 °C under relative humidity varied from 60% to 70%.

Figure S8. Nyquist plot of pelletized MOF-801 at 60 °C under relative humidity varied from 80% to 98%.

Table S3. Conductivity of pelletized MOF-801 at 70 oC from 60 to 98% RH.

| Relative humidity (%) | σ (S cm-1) |
| --- | --- |
| 60 | 2.60 x 10-7 |
| 70 | 1.05 x 10-6 |
| 80 | 2.45 x 10-6 |
| 90 | 7.06 x 10-6 |
| 95 | 2.86 x 10-5 |
| 98 | 1.31 x 10-3 |

Figure S9. Nyquist plot of pelletized MOF-801 at 70 °C under relative humidity varied from 60% to 98%

Table S4. Conductivity of pelletized MOF-801 at 80 oC from 60 to 98% RH.

| Relative humidity (%) | σ (S cm-1) |
| --- | --- |
| 60 | 6.25 x 10-7 |
| 70 | 2.22 x 10-6 |
| 80 | 4.69 x 10-6 |
| 90 | 1.28 x 10-5 |
| 95 | 3.34 x 10-5 |
| 98 | 1.58 x 10-3 |

Figure S10. Nyquist plot of pelletized MOF-801 at 80 °C under relative humidity varied from 60% to 70%.

Figure S11. Nyquist plot of pelletized MOF-801 at 80 °C under relative humidity varied from 80% to 98%.

Table S5. Conductivity of pelletized MOF-801 at 90 oC from 60 to 98 %RH.

| Relative humidity / % | σ / S cm-1 |
| --- | --- |
| 60 | 1.32 x 10-6 |
| 70 | 5.73 x 10-6 |
| 80 | 1.02 x 10-5 |
| 90 | 2.03 x 10-5 |
| 95 | 4.18 x 10-5 |
| 98 | 1.82 x 10-3 |

Figure S12. Nyquist plot of pelletized MOF-801 at 90 °C under relative humidity varied from 60% to 98%.

Section S3. Activation energy of materials under different relative humidities from 50 oC to 90 oC.

Table S6. Proton conduction of pelletized MOF-801 under 60, 70, 80, 90, 95 and 98 % RH from 50 to 90 oC.

| 60 %RH |  |
| --- | --- |
| Temperature (oC) | σ (S cm-1) |
| 50 | 4.49 x 10-8 |
| 60 | 8.84 x 10-8 |
| 70 | 2.60 x 10-7 |
| 80 | 6.25 x 10-7 |
| 90 | 1.32 x 10-6 |
| 70 %RH |  |
| Temperature (oC) | σ (S cm-1) |
| 50 | 2.08 x 10-7 |
| 60 | 4.55 x 10-7 |
| 70 | 1.05 x 10-6 |
| 80 | 2.22 x 10-6 |
| 90 | 5.73 x 10-6 |
| 80 %RH |  |
| Temperature (oC) | σ (S cm-1) |
| 50 | 6.01 x 10-7 |
| 60 | 1.12 x 10-6 |
| 70 | 2.45 x 10-6 |
| 80 | 4.69 x 10-6 |
| 90 | 1.02 x 10-5 |
| 90 %RH |  |
| Temperature (oC) | σ (S cm-1) |
| 50 | 1.53 x 10-6 |
| 60 | 3.56 x 10-6 |
| 70 | 7.06 x 10-6 |
| 80 | 1.28 x 10-5 |
| 90 | 2.03 x 10-5 |

| 95 %RH |  |
| --- | --- |
| Temperature (oC) | σ (S cm-1) |
| 50 | 2.08 x 10-5 |
| 60 | 2.40 x 10-5 |
| 70 | 2.86 x 10-5 |
| 80 | 3.34 x 10-5 |
| 90 | 4.18 x 10-5 |
| 98 %RH |  |
| Temperature (oC) | σ (S cm-1) |
| 50 | 8.84 x 10-4 |
| 60 | 1.05 x 10-3 |
| 70 | 1.31 x 10-3 |
| 80 | 1.58 x 10-3 |
| 90 | 1.82 x 10-3 |

Figure S13. Arrhenius plot of MOF-801 at 60, 70, 80, 90, 95 and 98 %R

Section S4. Stability of materials after ac impedance analysis.

Figure S14. PXRD pattern of MOF-801 before ac impedance analysis (black) in comparison with MOF-801 after ac impedance analysis (blue).

Computational methods

We utilize the package RASPA1 as implemented which based on Grand Canonical Monte Carlo 2,3 method to investigate water absorption isotherm and molecular dynamics (MD). The net atomic electrostatic charge of the framework structure via Bader charge analysis code based on DFT calculations which is developed by Henkelman researched group (Table S7).4-7 Lennard-Jones parameters which describe non-bonding interactions of water molecule and framework atoms are provided from semi-empirical force field which is appropriate for MOF applications,8 and we listed the above parameters in Table S8 for convenience. A Lennard-Jones cutoff of 12 Å was employed. Lorentz-Berthelot General2 the mixed rule is used for determining Lenard Jones parameters for potentials with different chemical species.

DFT calculations: MOF-801 configuration is optimized by ionic relaxation method at constant volume with the lattice parameter taken from the experimental data as a single crystal structure, a =17.8348 Å in the cubic space group, Pn3 (No. 201). Electronic structure calculations on a cubic unit-cell of MOF-801 (24 Zr, 128 O, 96 C and 48 H) are executed Vienna Ab Initio Simulation Package (VASP). 9-12 The Perdew-Burke-Ernzerhof13,14(PBE) parameterization is used to describe the exchange-correlation description within generalized-gradient approximations (GGA)15,16. Total energy difference between self-consistent-field (SCF) loops is set 10-5 eV and force convergence criterion is 10-2 eVÅ-1. We consider the cut-off energy of 400 eV which affords computational feasibility for a larger structure as MOF-801. The optimized structure is employed to analyze the net atomic electrostatic charge.

Molecular dynamics: Two MD simulation method NVT and NVT is employed at 50°C to research the proton transfer process in MOF-801. To enhance reliability for our calculation, the number of MD steps for the production run is 1× 106 for both above method and gap-time between each step is 0.5 fs. Six high-humidity point is considered including 60%, 70%, 80%, 90%, 95%, 98% which are examined by our experimental group. We verified that TIP4P/2005 force field appropriate to the water absorption calculation at several above high-humidity (Fig. S15). The number of water molecular in MOF-801 for MD process is calculated from the previous experimental adsorption results17 and is shown Table S9. For analyzing proton transfer process, every 500 steps we select one configuration in the last 25 × 104 steps from 1× 106 MD step. Consequently, there are a total of 500 configurations which allow us to perform reliable statistical results.

Isotherm calculation: The simulation temperature for isotherm curve is fixed at 55 °C which is the highest temperature for water uptake data in the previous experimental report.17 The pressure for system is calculated indirectly via humidity considering RH = P/Po, where RH is relative humidity (%), P and Po are pressure for system and saturated pressure of water at 55 °C, respectively. Simulations carried out using TIPnP water models to find out the water molecular model which is most appropriated with the experimental results. We suggest to employ three featured water model including: TIP3P,18 TIP4P/200519 and TIP5P.20 The electrostatic charge interactions were considered by the Ewald summation technique with an accuracy of 10-6 modeling long-interaction. In all our simulations, we perform 5 × 104 MC step of initial equilibration and 5 × 105 cycles for the production run. With 2 term of cycle for GCMC simulation, we recognize that only 3 × 105 cycles of assembling are needed to reach the saturation of water molecule into MOF-801.

Figure S15. Isotherm curve from GCMC simulation of MOF-801 with three force field of water molecular (TIP3P, TIP4P/2005, TIP5P) and experiment results at 55 °C.

| Atom | Charge | Atom | Charge | Atom | Charge | Atom | Charge | Atom | Charge | Atom | Charge |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Zr1 | 2.618 | O27 | -0.979 | O77 | -1.106 | O127 | -0.992 | C49 | 0.032 | H3 | 0.132 |
| Zr2 | 2.626 | O28 | -0.977 | O78 | -1.104 | O128 | -0.992 | C50 | -0.011 | H4 | 0.134 |
| Zr3 | 2.618 | O29 | -0.980 | O79 | -1.093 | C1 | 1.469 | C51 | -0.038 | H5 | 0.145 |
| Zr4 | 2.619 | O30 | -0.979 | O80 | -1.095 | C2 | 1.463 | C52 | -0.036 | H6 | 0.146 |
| Zr5 | 2.620 | O31 | -0.977 | O81 | -1.118 | C3 | 1.422 | C53 | 0.011 | H7 | 0.107 |
| Zr6 | 2.623 | O32 | -0.979 | O82 | -1.114 | C4 | 1.441 | C54 | -0.031 | H8 | 0.142 |
| Zr7 | 2.623 | O33 | -1.102 | O83 | -1.115 | C5 | 1.454 | C55 | -0.062 | H9 | 0.174 |
| Zr8 | 2.623 | O34 | -1.111 | O84 | -1.111 | C6 | 1.433 | C56 | 0.006 | H10 | 0.135 |
| Zr9 | 2.618 | O35 | -1.097 | O85 | -1.117 | C7 | 1.455 | C57 | -0.039 | H11 | 0.132 |
| Zr10 | 2.617 | O36 | -1.091 | O86 | -1.113 | C8 | 1.438 | C58 | -0.033 | H12 | 0.142 |
| Zr11 | 2.618 | O37 | -1.085 | O87 | -1.123 | C9 | 1.424 | C59 | 0.045 | H13 | 0.089 |
| Zr12 | 2.615 | O38 | -1.095 | O88 | -1.117 | C10 | 1.461 | C60 | 0.037 | H14 | 0.127 |
| Zr13 | 2.619 | O39 | -1.111 | O89 | -1.111 | C11 | 1.467 | C61 | -0.014 | H15 | 0.140 |
| Zr14 | 2.616 | O40 | -1.106 | O90 | -1.115 | C12 | 1.423 | C62 | 0.031 | H16 | 0.121 |
| Zr15 | 2.621 | O41 | -1.101 | O91 | -1.113 | C13 | 1.469 | C63 | -0.037 | H17 | 0.139 |
| Zr16 | 2.613 | O42 | -1.094 | O92 | -1.114 | C14 | 1.467 | C64 | -0.050 | H18 | 0.148 |
| Zr17 | 2.617 | O43 | -1.104 | O93 | -1.114 | C15 | 1.436 | C65 | -0.003 | H19 | 0.126 |
| Zr18 | 2.618 | O44 | -1.106 | O94 | -1.114 | C16 | 1.453 | C66 | -0.007 | H20 | 0.126 |
| Zr19 | 2.619 | O45 | -1.109 | O95 | -1.111 | C17 | 1.465 | C67 | -0.019 | H21 | 0.147 |
| Zr20 | 2.613 | O46 | -1.107 | O96 | -1.117 | C18 | 1.470 | C68 | -0.034 | H22 | 0.157 |
| Zr21 | 2.615 | O47 | -1.093 | O97 | -1.111 | C19 | 1.435 | C69 | -0.015 | H23 | 0.134 |
| Zr22 | 2.618 | O48 | -1.095 | O98 | -1.112 | C20 | 1.442 | C70 | -0.022 | H24 | 0.132 |
| Zr23 | 2.617 | O49 | -1.105 | O99 | -1.112 | C21 | 1.462 | C71 | -0.028 | H25 | 0.140 |
| Zr24 | 2.615 | O50 | -1.108 | O100 | -1.113 | C22 | 1.464 | C72 | -0.026 | H26 | 0.146 |
| O1 | -1.114 | O51 | -1.097 | O101 | -1.111 | C23 | 1.418 | C73 | -0.021 | H27 | 0.144 |
| O2 | -1.114 | O52 | -1.113 | O102 | -1.114 | C24 | 1.435 | C74 | -0.013 | H28 | 0.130 |
| O3 | -1.116 | O53 | -1.104 | O103 | -1.114 | C25 | 1.442 | C75 | -0.030 | H29 | 0.142 |
| O4 | -1.127 | O54 | -1.111 | O104 | -1.109 | C26 | 1.466 | C76 | -0.041 | H30 | 0.155 |
| O5 | -1.122 | O55 | -1.098 | O105 | -0.985 | C27 | 1.416 | C77 | -0.032 | H31 | 0.126 |
| O6 | -1.117 | O56 | -1.089 | O106 | -0.992 | C28 | 1.428 | C78 | -0.024 | H32 | 0.148 |
| O7 | -1.111 | O57 | -1.110 | O107 | -0.992 | C29 | 1.441 | C79 | 0.004 | H33 | 0.123 |
| O8 | -1.118 | O58 | -1.106 | O108 | -0.992 | C30 | 1.417 | C80 | -0.029 | H34 | 0.139 |
| O9 | -1.118 | O59 | -1.090 | O109 | -0.992 | C31 | 1.465 | C81 | -0.029 | H35 | 0.141 |
| O10 | -1.119 | O60 | -1.092 | O110 | -0.989 | C32 | 1.462 | C82 | -0.055 | H36 | 0.107 |
| O11 | -1.112 | O61 | -1.093 | O111 | -0.987 | C33 | 1.432 | C83 | -0.014 | H37 | 0.139 |
| O12 | -1.111 | O62 | -1.084 | O112 | -0.987 | C34 | 1.413 | C84 | 0.095 | H38 | 0.091 |
| O13 | -1.115 | O63 | -1.109 | O113 | -0.987 | C35 | 1.471 | C85 | -0.023 | H39 | 0.136 |
| O14 | -1.115 | O64 | -1.092 | O114 | -0.986 | C36 | 1.444 | C86 | -0.010 | H40 | 0.142 |
| O15 | -1.123 | O65 | -1.092 | O115 | -0.981 | C37 | 1.474 | C87 | -0.016 | H41 | 0.127 |
| O16 | -1.122 | O66 | -1.096 | O116 | -0.984 | C38 | 1.447 | C88 | -0.036 | H42 | 0.108 |
| O17 | -1.117 | O67 | -1.109 | O117 | -0.990 | C39 | 1.428 | C89 | -0.021 | H43 | 0.142 |
| O18 | -1.112 | O68 | -1.099 | O118 | -0.989 | C40 | 1.436 | C90 | -0.021 | H44 | 0.131 |
| O19 | -1.118 | O69 | -1.114 | O119 | -0.992 | C41 | 1.456 | C91 | -0.031 | H45 | 0.147 |
| O20 | -1.121 | O70 | -1.099 | O120 | -0.988 | C42 | 1.448 | C92 | -0.050 | H46 | 0.161 |
| O21 | -1.117 | O71 | -1.085 | O121 | -0.992 | C43 | 1.421 | C93 | -0.022 | H47 | 0.146 |
| O22 | -1.113 | O72 | -1.094 | O122 | -0.994 | C44 | 1.458 | C94 | -0.021 | H48 | 0.135 |
| O23 | -1.111 | O73 | -1.112 | O123 | -0.993 | C45 | 1.473 | C95 | -0.022 | H3 | 0.139 |
| O24 | -1.122 | O74 | -1.114 | O124 | -0.988 | C46 | 1.467 | C96 | -0.034 | H4 | 0.150 |
| O25 | -0.977 | O75 | -1.096 | O125 | -0.995 | C47 | 1.425 | H1 | 0.132 | H5 | 0.132 |
| O26 | -0.977 | O76 | -1.093 | O126 | -0.988 | C48 | 1.426 | H2 | 0.134 | H6 | 0.134 |

Table S7. The net atomic electrostatic charge of MOF-801 is analyzed from DFT calculation.

Table S8. Lennard-Jones parameters for MOF-801 and water molecular for TIP3P18, TIP4P/200519, TIP5P20 (with UFF force field for Oframework).

| Atom | σ (Å) | Ɛ (kB) |
| --- | --- | --- |
| Oframework | 3.033 | 48.158 |
| Cframework | 3.473 | 47.856 |
| Hframework | 2.846 | 7.648 |
| Zrframework | 2.783 | 34.722 |
| Owater-TIP3P | 3.150 | 76.541 |
| Owater-TIP4P/2005 | 3.151 | 93.199 |
| Owater-TIP5P | 3.120 | 80.510 |

Table S9. Number of water molecular is calculate from water uptake which is reference from the experimental adsorption results17 for MOF-801 at 50°C

| Humidity | 60% | 70% | 80% | 90% | 95% | 98% |
| --- | --- | --- | --- | --- | --- | --- |
| Water-uptake (cm3/g) (The experimental results) | 419 | 452 | 473 | 499 | 506 | 509 |
| Number of water molecular | 102 | 109 | 114 | 121 | 122 | 123 |

| Hydrogen bond Type | Strong | Moderate | Weak |
| --- | --- | --- | --- |
| Interaction Type | Strongly Covalent | Mostly Electrostatic | Electrostatic/dispersion |
| Bond lengths Odonor-Oaceptor (Å) | 2.2 – 2.5 | 2.5 – 3.2 | 3.2 – 4.0 |
| Bond angles (Degree) | 170 - 180 | >130 | > 90 |

Table S10. Strong, moderate and weak hydrogen bonds following the classification of Jeffrey.21

Table S11. Average Number of Hydrogen bond and Bond length in a unit-cell of MOF-801 at the several humidity from NVT simulation.

| Humidity |  |  | 60% | 70% | 80% | 90% | 95% | 98% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Hydrogen Bond Types | Strong | Average number of hydrogen bond | 0.06 | 0.07 | 0.06 | 0.06 | 0.12 | 0.11 |
|  |  | Average bond length Odonor-Oaceptor (Å) | 2.48 | 2.48 | 2.47 | 2.47 | 2.48 | 2.47 |
|  | Moderate | Average number of hydrogen bond | 121.42 | 129.78 | 138.06 | 144.70 | 148.02 | 148.14 |
|  |  | Average bond length Odonor-Oaceptor (Å) | 2.80 | 2.81 | 2.81 | 2.79 | 2.79 | 2.78 |
|  | Weak | Average number of hydrogen bond | 93.5 | 112.51 | 121.64 | 144.96 | 141.36 | 149.96 |
|  |  | Average bond length Odonor-Oaceptor (Å) | 3.63 | 3.61 | 3.60 | 3.60 | 3.60 | 3.60 |

References

D. Dubbeldam, S. Calero, D. E. Ellis, R. Q. Snurr, Mol. Simul., 2016, 42, 81.

M. P. Allen and D. J. Tildesley, Oxford Science Publications, Clarendon Press, 1987.

O. P. A. Partykiejew, S. Sokolowski, Wiley-VCH GmbH & Co. KGaA, Weinheim, 2016.

W. Tang, E. Sanville, G. Henkelman, J. Phys.: Condens. Matter, 2009, 21, 084204.

E. Sanville, S. D. Kenny, R. Smith, G. Henkelman, J. Comp. Chem., 2007, 28, 899.

G. Henkelman, A. Arnaldsson, H. Jónsson, Comput. Mater. Sci., 2006, 36, 354.

M. Yu, D. R. Trinkle, J. Chem. Phys., 2011, 134, 064111.

J. E. Jones, Proc. Royal Soc. Lond. A, 1924, 106, 463.

G. Kresse, J. Hafner, Phys. Rev. B, 1993, 47, 558-561.

G. Kresse, J. Hafner, Phys. Rev. B, 1994, 49, 14251-14269.

G. Kresse, J. Furthmüller, Comput. Mater. Sci., 1996, 6, 15-50.

G. Kresse, J. Furthmüller, Phys. Rev. B, 1996, 54, 11169-11186.

J. P. Perdew, K. Burke, M. Ernzerhof, Phys. Rev. Lett., 1996, 77, 3865-3868.

J. P. Perdew, K. Burke, M. Ernzerhof, [Phys. Rev. Lett.,1996, 77, 3865]. Phys. Rev. Lett., 1997, 78, 1396-1396.

P. E. Blöchl, Phys. Rev. B, 1994, 50, 17953-17979.

G. Kresse, D. Joubert, Phys. Rev. B, 1994, 59, 1758-1775.

H. Furukawa, F. Gandara, Y. B. Zhang, J. Jiang, W. L. Queen, M. R. Hudson, O. M. Yaghi, J. Am. Chem. Soc., 2014, 136, 4369.

D. J. Price, C. L. A Brooks, J. Chem. Phys., 2004, 121, 10096.

J. L. F. Abascal, C. Vega, J. Chem. Phys., 2005, 123, 234505.

S. W. Rick, J. Chem. Phys., 2004, 120, 6085.

G. A. Jeffrey, An Introduction to Hydrogen Bonding, Oxford University Press, Oxford, 1997.